Supplemental Materials

Inheritance factor on the physical properties in metallic glasses

Weiming Yang1, †, Jiawei Li2,†, Hongyang Li1, Haishun Liu3, *, Jinyong Mo3, Si Lan4, 5, Maozhi Li6, Xun-Li Wang5, 7, Jürgen Eckert8, 9 and Juntao Huo2, *

1	School of Mechanics and Civil Engineering, State Key Laboratory for Geomechanics and Deep Underground Engineering, China University of Mining and Technology, Xuzhou 221116, China

2	CAS Key Laboratory of Magnetic Materials and Devices, Zhejiang Province Key Laboratory of Magnetic Materials and Application Technology, Ningbo Institute of Materials Technology and Engineering, Chinese Academy of Sciences, Ningbo, Zhejiang 315201, China

3	School of Materials and Physics, China University of Mining and Technology, Xuzhou 221116, China

4	Herbert Gleiter Institute of Nanoscience, Nanjing University of Science and Technology, 200 Xiaolingwei Avenue, Nanjing 210094, China

5	Department of Physics, City University of Hong Kong, 83 Tat Chee Avenue, Hong Kong, China

6	Department of Physics, Beijing Key Laboratory of Opto-electronic Functional Materials and Micro-nano Devices, Renmin University of China, Beijing 100872, China

7	Center for Neutron Scattering, City University of Hong Kong Shenzhen Research Institute, 8 Yuexing 1st Road, Shenzhen Hi-Tech Industrial Park, Shenzhen 518057, China

8	Erich Schmid Institute of Materials Science, Austrian Academy of Science, 8700 Leoben, Austria

9	Department of Materials Science, Chair of Materials Physics, Montanuniversität Leoben, 8700 Leoben, Austria

† These authors made equal contributions.

* To whom correspondence should be addressed. liuhaishun@cumt.edu.cn (H. S. Liu) and huojuntao@nimte.ac.cn (J. T. Huo)

Table S1 Experimental Young’s modulus (E) and shear modulus (G) for MGs and their components Cu and Zr. Also listed are the ratios of MGs to Zr and Cu in terms of elastic modulus, respectively.

| Numbers | Compositions | E (GPa) | G (GPa) | References |
| --- | --- | --- | --- | --- |
|  |  | MGs | EMG/EZr | EMG/ECu | MGs | GMG/GZr | GMG/GCu |  |
| 1 | Cu50Zr45Al5 | 91.2 | 0.93 | 0.70 | 33.3 | 0.95 | 0.69 | 1 |
| 2 | (Cu46Zr42Al7Y5)96Sn4 | 92.9 | 0.95 | 0.71 | 34.4 | 0.98 | 0.72 | 1 |
| 3 | Cu60Zr20Hf10Ti10 | 101.1 | 1.03 | 0.78 | 36.9 | 1.05 | 0.77 | 2 |
| 4 | Cu60Zr29Ti10Sn1 | 95.5 | 0.97 | 0.73 | 36.6 | 1.04 | 0.76 | 1 |
| 5 | (Cu50Zr50)94Al6 | 92.4 | 0.94 | 0.71 | 33.8 | 0.97 | 0.70 | 3 |
| 6 | (Cu50Zr50)92Al8 | 93.7 | 0.96 | 0.72 | 34.3 | 0.98 | 0.71 | 3 |
| 7 | (Cu50Zr50)90Al10 | 99.1 | 1.01 | 0.76 | 36.3 | 1.04 | 0.76 | 1 |
| 8 | (Cu50Zr50)90Al7Gd3 | 90.6 | 0.92 | 0.70 | 32.9 | 0.94 | 0.70 | 1 |
| 9 | Cu60Zr30Ti10 | 93.0 | 0.95 | 0.72 | 33.8 | 0.97 | 0.70 | 4 |
| 10 | Cu60Zr32.5Ti7.5 | 90.0 | 0.92 | 0.69 | 32.8 | 0.94 | 0.68 | 5 |
| 11 | Cu47Zr11Ti34Ni8 | 97.0 | 0.99 | 0.75 | 35.5 | 1.01 | 0.74 | 5 |
| 12 | Cu68Zr32 | 89.6 | 0.91 | 0.69 | 32.0 | 0.91 | 0.67 | 6 |
| 13 | Cu64Zr36 | 92.0 | 0.94 | 0.71 | 34.0 | 0.97 | 0.71 | 7 |
| 14 | Cu50Zr50 | 85.0 | 0.88 | 0.65 | 31.3 | 0.89 | 0.65 | 7 |
| 15 | Cu46Zr54 | 83.5 | 0.85 | 0.64 | 30.0 | 0.86 | 0.63 | 7 |
| Mean |  | 0.94 | 0.71 |  | 0.97 | 0.71 |  |

Table S1 summarizes experimental data of Young’s moduli (E) and shear moduli (G) for a variety of MGs 1-8 based on Cu and/or Zr.

It is surprising that these physical properties of glasses are close to those of Zr, not their major component Cu. This is unusual because the minor component Zr seems to be responsible for their properties instead of the major component Cu. For instance, E of Cu64Zr36 glasses is 92.0 GPa, which is very close to that of pure polycrystalline Zr (98.0 GPa) 9, whereas, this value is much smaller than that of Cu (130 GPa) 9. As for G, Cu64Zr36 glasses have values of 34.0 GPa, which are also around that of Zr (35.9 GPa), but significantly smaller than that of Cu (48.3 GPa) 9. The average E of the MGs listed in Table I is found to be ~95 % of Zr, while for G, the ratio is ~97 %. In view of the analytical uncertainties ~5% 10 of experiments obtained by ultrasonic measurements, one can conclude that the elastic moduli of MGs in Table 1 are primarily determined by the Zr component, while a relatively small fraction comes from another components. According to the previous research 11,12, the basic physical properties, such as thermal stability, magnetic and mechanical properties, etc., are directly related to the elastic moduli of MGs. Therefore, assumption may be made as some basic physical properties mainly inherit from their individual component in spite of the structural and chemical complexity of MGs.

Figure S1 XRD (a) and DSC (b) traces of glassy samples.

The XRD patterns display broad diffraction maxima, which are the characteristic of glassy structure. The DSC traces exhibit endothermic event characteristics of the glass transition from glassy solids into supercooled liquid, followed by the crystallization exothermic reactions, which enable them to confirm the glassy nature of the MGs.

Figure S2 Spin polarized total and partial EDOS of Fe74Mo6P13C7 MG. (a) Mo EDOS, (b) P EDOS, (c) C EDOS, and (d) Fe EDOS and total MG.

Table S2. Summary of the structural information and mechanical properties of MGs, including first diffraction peak on the S(q1) curves, yield strength σy, and elastic moduli E and G.

| Numbers | Composition | q1 (Å−1) | σy (GPa) | G (GPa) | E (GPa) | Tg (K) | References |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Al89La6Ni5 | 2.541 | 1.033 |  |  |  | 13-15 |
| 2 | Au49Ag5.5Pd2.3Cu26.9Si16.3 | 2.836 | 1.12 | 26.5 | 74.4 | 401 | 16-18 |
| 3 | Ca65Mg15Zn20 | 2.174 | 0.364 | 10.1 | 22.4 | 375 | 19,20 |
| 4 | Ca60Mg15Cu25 | 2.239 | 0.252 |  |  | 396 | 21,22 |
| 5 | Cu65Zr35 | 2.822 | 2.019 |  |  | 750 | 23-25 |
| 6 | Cu64Zr36 | 2.838 | 1.944 | 34 | 92 | 744 | 23,24,26-28 |
| 7 | Cu61.4Zr38.6 | 2.801 | 1.87 |  |  |  | 23,24 |
| 8 | Cu56Zr44 | 2.763 | 1.82 |  |  | 690 | 23,24,29 |
| 9 | Cu50Zr50 | 2.719 | 1.772 | 31.3 | 85 | 733 | 23,30-32 |
| 10 | Cu46Zr54 | 2.674 | 1.5926 | 30 | 83.5 | 696 | 26,33 |
| 11 | Cu40Zr60 | 2.656 | 1.333 |  |  | 625 | 34,35 |
| 12 | Cu33.3Zr66.7 | 2.564 | 1.17 |  |  | 610 | 36 |
| 13 | Cu48Zr48Al4 | 2.71 | 1.65 | 32.4 | 88.7 | 689 | 30,31,36,37 |
| 14 | Cu47.5Zr47.5Al5 | 2.72 | 1.742 | 33 | 87 | 693 | 30,31,36,37 |
| 15 | Cu47Zr47Al6 | 2.72 | 1.834 | 33.8 | 92.4 | 700 | 36,38 |
| 16 | Cu46Zr46Al8 | 2.73 | 1.926 | 34.3 | 93.7 | 701 | 36,38,39 |
| 17 | Cu47Ti33Zr11Ni8Si1 | 2.875 | 2 | 38.3 | 100 | 692 | 40 41 |
| 18 | Cu47Ti33Zr11Ni8Fe1 | 2.86 | 2.008 | 39 | 102 |  | 41 42 |
| 19 | Co43Fe20Ta5.5B31.5 | 3.186 | 5.147 | 102.7 | 268 | 910 | 36,43-46 |
| 20 | Fe76.0C7.0Si3.3B5.0P8.7 | 3.025 | 3 | 63.2 | 165 |  | 36,47 |
| 21 | Fe75.7C7.0Si3.3B5.0P8.7Cu0.3 | 3.025 | 3.5 | 70.58 | 184.2 |  | 36,47 |
| 22 | [(Fe0.5Co0.5)0.75B0.2Si0.05]96Nb4 | 3.156 | 4.21 | 80.46 | 210 | 830 | 48 49 |
| 23 | Fe40Ni40P14B6 | 2.922 | 2.23 |  |  | 659 | 50 51 |
| 24 | Fe66Nb4B30 | 3.082 | 4 |  |  | 845 | 52 53 |
| 25 | Mg65Cu25Gd10 | 2.519 | 0.83 | 19.3 | 50.6 | 421 | 54 16 |
| 26 | Mg65Cu25Tb10 | 2.52 | 0.76 | 19.6 | 51.3 | 417 | 55 56 16 |
| 27 | Mg61Cu28Gd11 | 2.526 | 1.075 |  |  | 422 | 57 58 |
| 28 | Ni60Nb37Sn3 | 2.944 | 2.8 | 58.6 | 198.6 | 895 | 59 |
| 29 | Ni60Nb35Sn5 | 2.962 | 2.5 | 54.1 | 183.2 | 885 | 59 |
| 30 | Ni60Sn6(Nb0.8Ta0.2)34 | 2.93 | 3.5 | 59.41 | 161.3 | 880 | 60 61 |
| 31 | Ni60Sn6(Nb0.6Ta0.4)34 | 2.917 | 3.58 | 60.1 | 163.7 | 884 | 60 61 |
| 32 | Ni60Pd20P20 | 2.99 | 2.0 |  |  | 594 | 62-64 |
| 33 | Ni60Pd20P17B3 | 2.99 | 2.022 | 38 | 106 |  | 63 64 |
| 34 | Pd80Si20 | 2.727 | 1.3 | 33.4 | 94.5 | 607 | 50 65 |
| 35 | Pd40Ni40P20 | 2.886 | 1.65 | 38.6 | 108 | 583 | 66-69 16 |
| 36 | Pd40Cu30Ni10P20 | 2.9 | 1.72 | 34.5 | 92 | 593 | 67-69 16 |
| 37 | Ti40Zr25Ni3Cu12Be20 | 2.72 | 1.8 | 35.5 | 96.2 | 658 | 16,36 |
| 38 | Zr57Ti5Cu20Ni8Al10 | 2.602 | 1.65 | 30.1 | 82 | 657 | 16,70 |
| 39 | Zr55Cu35Al10 | 2.649 | 1.74 |  |  |  | 71 |
| 40 | Zr41Ti14Cu12.5Ni10Be22.5 | 2.84 | 1.86 | 37.4 | 101.3 | 620 | 16,72 |
| 41 | Zr53.7Cu28.5Ni9.4Al8.4 | 2.675 | 1.85 |  | 85 |  | 36 |
| 42 | Zr52.5Ti5Cu17.9Ni14.6Al10 | 2.658 | 1.86 | 32.3 | 88.6 | 684 | 16,34 |
| 43 | Zr64.13Cu15.75Ni10.12Al10 | 2.58 | 1.721 | 28.46 | 78.41 | 640 | 16,73 |
| 44 | Zr62Al8Ni13Cu17 | 2.585 | 1.46 |  |  |  | 74 |
| 45 | Zr46Cu37.6Ag8.4Al8 | 2.76 | 1.716 | 33.8 | 92.4 | 705 | 36,75 |
| 46 | Zr53.8Cu31.6Ag7Al7.6 | 2.71 | 1.518 | 29.9 | 82 | 710 | 75 |
| 47 | Zr48Cu36Al8Ag8 | 2.66 | 1.85 | 44 | 115 | 720 | 36,76 |
| 48 | La62Al14(Cu5/6Ag1/6)14(Ni1/2Co1/2))10 | 2.2 | 0.65 | 13 | 35 |  | 16,77,78 |
| 49 | Y55Al25Co20 | 2.23 | 1.203 |  |  | 633 | 16,34,79 |
| 50 | La55Al25Co20 | 2.32 | 0.989 | 15.42 | 40.9 | 477 | 16,34,79 |
| 51 | Pr55Al25Co20 | 2.35 | 1.007 | 17.35 | 45.9 | 509 | 16,34,79 |
| 52 | Nd55Al25Co20 | 2.33 | 0.996 |  |  | 525 | 16,34,79 |
| 53 | Gd55Al25Co20 | 2.36 | 0.734 |  |  | 585 | 16,34,79 |
| 54 | Tb55Al25Co20 | 2.35 | 0.834 | 22.85 | 59.53 | 612 | 16,34,79 |
| 55 | Dy55Al25Co20 | 2.42 | 0.717 | 23.52 | 61.36 | 635 | 16,34,79 |
| 56 | Ho55Al25Co20 | 2.39 | 0.869 | 25.42 | 66.64 | 649 | 16,34,79 |
| 57 | Er55Al25Co20 | 2.36 | 1.117 | 27.08 | 70.72 | 663 | 16,34,79 |

Table S3 Experimental data on mechanical properties (yield strength σy, elastic modulus E and shear modulus G), valence electron density ρ, and glass transition temperature Tg of metallic glasses.

| Numbers | Compositions | (GPa) | E (GPa) | G (GPa) | ρ (e/Å3) | Tg (K) | References |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Fe60Co20B20 |  | 172.6 | 65.1 | 0.3506 |  | 80 |
| 2 | Fe40Co40B20 |  | 174.2 | 65 | 0.3552 | 655 | 80,81 |
| 3 | Fe71Nb6B23 | 4.85 |  |  | 0.3410 | 819 | 82,83 |
| 4 | Fe56.05Co13.45Nb5.5B25 | 4.5 |  |  | 0.3299 | 821 | 84 |
| 5 | Fe75.924Si9.5904B8.3916P5.994Cu0.1 | 3.3 |  |  | 0.3044 | 785 | 85 |
| 6 | [(Fe0.5Co0.5)0.75B0.2Si0.05]96Nb4 | 4.21 | 210 | 80.46 | 0.3375 | 830 | 86 |
| 7 | Fe40Ni40P14B6 | 2.23 |  |  | 0.3111 | 659 | 87,88 |
| 8 | Fe66Nb4B30 | 4.0 |  |  | 0.3454 | 845 | 89,90 |
| 9 | (Fe0.75B0.2Si0.05)96Nb4 | 3.16 | 180 |  | 0.3302 | 835 | 86 |
| 10 | Co74Fe6B20 |  | 175.4 | 66.4 | 0.3633 |  | 80 |
| 11 | Co60Fe20B20 |  | 174.1 | 65.7 | 0.3599 | 705 | 80 |
| 12 | Ni45Ti20Zr25Al10 | 2.37 | 109.3 | 40.2 | 0.2322 | 733 | 91 |
| 13 | Ni60Nb12.5Zr20Al5Ti2.5 | 2.885 |  |  | 0.2701 | 836 | 92 |
| 14 | Ni60Nb10Zr20Al5Ti5 | 2.885 |  |  | 0.2677 | 826 | 92 |
| 15 | Ni40Ti17Zr28Al10Cu5 | 2.3 | 127.6 | 47.3 | 0.2262 | 762 | 91 |
| 16 | Ni62.5Zr20Nb15Pd2.5 | 2.85 |  |  | 0.2794 | 867 | 93 |
| 17 | Ni60Zr20Nb15Pd5 | 2.81 |  |  | 0.2776 | 873 | 93 |
| 18 | Ni52.5Zr20Nb15Pd12.5 | 2.75 |  |  | 0.2723 | 861 | 93 |
| 19 | Ni53Nb20Ti10Zr8Co6Cu3 |  |  |  | 0.2812 | 846 | 94 |
| 20 | Ni60Pd20P20 | 1.78 | 114 |  | 0.2856 | 594 | 95-97 |
| 21 | Ni60Pd20P17B3 | 2.022 | 106 | 38 | 0.2930 |  | 96,97 |
| 22 | Ni50Nb50 | 2.26 |  | 48.1 | 0.3112 | 875 | 10,98 |
| 23 | Mg65Cu25Y10 | 0.68 | 50.1 | 18.9 | 0.1100 | 419 | 99 |
| 24 | Mg58.5Cu30.5Y11 | 1.22 | 53.9 | 20.4 | 0.1159 |  | 100 |
| 25 | Mg65Cu20Y15 | 0.82 |  |  | 0.1048 | 420 | 10 |
| 26 | Ti45Zr20Be35 | 1.86 | 96.8 | 35.7 | 0.1942 | 597 | 101 |
| 27 | Ti40Zr25Be35 | 1.72 | 99.6 | 37.2 | 0.1910 | 598 | 101 |
| 28 | Ti30Zr35Be35 |  | 98.5 | 36.4 | 0.1848 | 595 | 101 |
| 29 | Ti50Ni42Cu8 | 2.08 |  |  | 0.2558 | 657 | 102 |
| 30 | Ti39.6Zr9.9Cu35.64Pd13.86Nb1 | 2.05 |  |  | 0.2174 | 675 | 103 |
| 31 | Ti38Zr9.5Cu34.2Pd13.3Nb5 | 2.05 | 80 |  | 0.2202 | 675 | 103 |
| 32 | Ti40Zr25Ni3Cu12Be20 | 1.8 | 96.2 | 35.5 | 0.1958 | 658 | 104 |
| 33 | Zr45Cu45Al10 |  |  | 35.4 | 0.1876 | 703 | 105 |
| 34 | Zr47.5Cu47.5Al5 | 1.547 | 87 | 33 | 0.1875 | 698 | 106 |
| 35 | Zr64Cu26Al10 | 1.710 |  | 28.7 | 0.1721 | 662 | 107 |
| 36 | Zr65Cu15Ni10Al10 | 1.45 | 82.96 | 30.27 | 0.1772 | 652 | 5,108 |
| 37 | Zr62Cu15.5Ni12.5Al10 |  | 79.65 | 28.89 | 0.1810 | 643 | 108 |
| 38 | Zr53Cu20Ni12Al10Ti5 |  | 87.58 | 32.12 | 0.1857 |  | 10 |
| 39 | Zr55Cu20Ni10Al10Ti5 | 1.63 | 85 | 31 | 0.1827 | 657 | 109 |
| 40 | Zr57Cu20Ni8Al10Ti5 | 1.65 | 82 | 30.1 | 0.1798 | 657 | 110 |
| 41 | Zr59Cu20Ni8Al10Ti3 | 1.69 | 91 |  | 0.1792 |  | 111 |
| 42 | Zr57Nb5Cu15.4Ni12.6Al10 | 1.8 | 87.3 | 31.98 | 0.1872 | 687 | 112 |
| 43 | Zr55Cu35Al10 | 1.74 |  |  | 0.1788 |  | 113 |
| 44 | Zr41Ti14Cu12.5Ni10Be22.5 | 1.86 | 101.3 | 37.4 | 0.1943 | 625 | 104,114 |
| 45 | Zr53.7Cu28.5Ni9.4Al8.4 | 1.85 | 85 |  | 0.1865 |  | 115 |
| 46 | Zr52.5Ti5Cu17.9Ni14.6Al10 | 1.86 | 88.6 | 32.3 | 0.1884 | 684 | 104,116 |
| 47 | Zr64.13Cu15.75Ni10.12Al10 | 1.721 | 78.41 | 28.46 | 0.1779 | 640 | 104,108 |
| 48 | Zr62Cu17Ni13Al8 | 1.46 |  |  | 0.1822 |  | 117 |
| 49 | Zr46.75Ti8.25Cu7.5Ni10Be27.5 | 1.83 | 83 | 37.2 | 0.1899 | 623 | 118,119 |
| 50 | Cu68Zr32 |  | 89.6 | 32 | 0.2060 | 733 | 6 |
| 51 | Cu64Zr36 | 1.944 | 92.0 | 34 | 0.2016 | 744 | 120 |
| 52 | Cu50Zr50 | 1.772 | 83.2 | 30 | 0.1878 | 733 | 106,120 |
| 53 | Cu46Zr54 | 1.5926 | 83.5 | 30 | 0.1843 | 696 | 120,121 |
| 54 | Cu60Zr30Ti10 |  | 93 | 33.8 | 0.2039 | 706 | 122 |
| 55 | Cu60Zr32.5Ti7.5 | 2.20 | 90 | 32.8 | 0.2022 |  | 5 |
| 56 | Cu54Zr42.5Al3.5 |  | 81.3 | 29.2 | 0.1929 | 717 | 123 |
| 57 | Cu53.2Zr41.8Al5 |  | 85.6 | 30.9 | 0.1928 | 721 | 123 |
| 58 | Cu51.5Zr40.5Al8 |  | 87.4 | 31.6 | 0.1924 | 730 | 123 |
| 59 | Cu50Zr45Al5 | 1.89 | 91.2 | 33.3 | 0.1897 | 701 | 5 |
| 60 | Cu47Zr11Ti34Ni8 | 1.6 |  |  | 0.2214 | 672 | 5 |
| 61 | Cu65Zr35 | 2.019 |  |  | 0.2026 | 781 | 124,125 |
| 62 | Cu61.4Zr38.6 | 1.87 |  |  | 0.1988 |  | 124,125 |
| 63 | Cu56Zr44 | 1.82 |  |  | 0.1934 | 690 | 124-126 |
| 64 | Cu40Zr60 | 1.333 |  |  | 0.1794 | 625 | 127,128 |
| 65 | Cu33.3Zr66.7 | 1.17 |  |  | 0.1744 | 610 | 128 |
| 66 | Cu48Zr48Al4 | 1.65 | 88.7 | 32.4 | 0.1875 | 689 | 106,129,130 |
| 67 | Cu47.5Zr47.5Al5 | 1.742 | 87 | 33 | 0.1875 | 693 | 106,129,130 |
| 68 | Cu47Zr47Al6 | 1.834 | 92.4 | 33.8 | 0.1874 | 700 | 106,129,131 |
| 69 | Cu46Zr46Al8 | 1.926 | 93.7 | 34.3 | 0.1873 | 701 | 131,132 |
| 70 | Cu47Ti33Zr11Ni8Si1 | 1.881 | 100 | 38.3 | 0.2181 | 692 | 133,134 |
| 71 | Cu47Ti33Zr11Ni8Fe1 | 2.008 | 102 | 39 | 0.2226 |  | 134,135 |
| 72 | Cu55Zr30Ti10Co5 | 2.31 | 130 |  | 0.2075 | 714 | 10 |
| 73 | Cu60Zr40 | 1.92 | 107 |  | 0.1974 | 710 | 136 |
| 74 | Pt57.5Cu14.7Ni5.3P22.5 | 1.4 | 94.8 | 33.3 | 0.2376 | 508 | 137 |
| 75 | Pt60Ni15P25 |  | 96 | 33.8 | 0.2428 | 485 | 10 |
| 76 | Pt60Cu16Co2P22 | 1.1 | 96 |  | 0.2359 | 506 | 10 |
| 77 | Pd77.5Cu6Si16.5 | 1.4 | 89.7 | 31.8 | 0.2556 | 633 | 5 |
| 78 | Pd40Cu40P20 | 1.7 | 93 | 33.2 | 0.2360 | 590 | 138 |
| 79 | Pd79Cu6Si10P5 | 1.475 | 82 |  | 0.2545 | 615 | 139 |
| 80 | Pd42.5Cu30Ni7.5P20 |  | 101.9 | 36.5 | 0.2428 | 560 | 140,141 |
| 81 | Pd80Si20 | 1.3 | 94.5 | 33.4 | 0.2535 | 607 | 5,138,142 |
| 82 | Pd40Ni40P20 | 1.65 | 108 | 38.6 | 0.2702 | 583 | 5,138,142 |
| 83 | Pd40Cu30Ni10P20 | 1.72 | 92 | 34.5 | 0.2444 | 593 | 5,138,142 |
| 84 | Pd80P20 |  |  | 33.1 | 0.2440 | 607 | 5,138,142 |
| 85 | Pd64Fe16P20 |  |  | 27.1 | 0.2516 | 630 | 5,138,142 |
| 86 | La55Al25Cu10Ni5Co5 | 0.5 | 41.9 | 15.6 | 0.1124 | 466 | 143 |
| 87 | La55Al25Co20 | 0.99 | 40.9 | 15.42 | 0.1185 | 477 | 144 |
| 88 | La55Al15Ni10P20 | 0.5 | 41 |  | 0.1106 |  | 10 |
| 89 | Al89La6Ni5 | 1.033 |  |  | 0.1735 |  | 145,146 |
| 90 | Y55Al25Co20 | 1.203 |  |  | 0.1304 | 635 | 104,127,144 |

Table S4 Summary of elastic moduli for some MGs.

| Numbers | Compositions | DOS inherited element | E (GPa) | G (GPa) | References |
| --- | --- | --- | --- | --- | --- |
|  |  |  | MGs | EMG/Ebas | EMG/EDOS | MGs | GMG/Gbas | GMG/GDOS |  |
| 1 | Cu60Zr20Hf10Ti10 | Zr | 101 | 0.78 | 1.03 | 36.9 | 0.77 | 1.05 | 9 |
| 2 | Cu68Zr32 |  | 89.6 | 0.69 | 0.92 | 32 | 0.67 | 0.91 | 147 |
| 3 | Cu64Zr36 |  | 92.0 | 0.71 | 0.94 | 34 | 0.71 | 0.97 | 147 |
| 4 | Cu50Zr50 |  | 83.2 | 0.64 | 0.85 | 30 | 0.63 | 0.86 | 147 |
| 5 | Cu46Zr54 |  | 83.5 | 0.85 | 0.85 | 30 | 0.86 | 0.86 | 147 |
| 6 | (Ce10La90)68Al10Cu20Co2 | Ce | 30.4 | 0.82 | 0.91 | 11.2 | 0.75 | 0.83 | 148 |
| 7 | (Ce20La80)68Al10Cu20Co2 |  | 30.7 | 0.83 | 0.92 | 11.3 | 0.76 | 0.84 | 148 |
| 8 | (Ce30La70)68Al10Cu20Co2 |  | 31.4 | 0.85 | 0.94 | 11.6 | 0.78 | 0.86 | 148 |
| 9 | (Ce40La60)68Al10Cu20Co2 |  | 30.4 | 0.82 | 0.91 | 11.2 | 0.75 | 0.83 | 148 |
| 10 | (Ce50La50)68Al10Cu20Co2 |  | 31.3 | 0.85 | 0.93 | 11.6 | 0.78 | 0.86 | 148 |
| 11 | (Ce70La30)68Al10Cu20Co2 |  | 31.8 | 0.94 | 0.94 | 11.9 | 0.85 | 0.85 | 148 |
| 12 | (Ce80La20)68Al10Cu20Co2 |  | 31.1 | 0.94 | 0.91 | 11.6 | 0.86 | 0.86 | 148 |
| 13 | Mg65Cu25Gd10 | Gd | 50.6 | 1.12 | 0.92 | 19.3 | 1.14 | 0.88 | 149 |
| 14 | Mg60Cu25Zn5Gd10 |  | 54.0 | 1.20 | 0.98 | 20.6 | 1.21 | 0.94 | 149 |
| 15 | Y27.5Tm27.5Al25Co20 | Y | 68.0 | — | 1.06 | 25.8 | — | 1.05 | 150 |
| 16 | Zn20Ca20Sr20Yb20Li11Mg9 | Sr | 16.0 | — | 0.89 | 6.3 | — | 1.03 | 151 |
| 17 | Zr20Ti20Hf20Be20Cu20 | Ti | 111 | — | 0.96 |  |  |  | 152 |
| 18 | Zr20Ti20Hf20Be20Cu15Ni5 |  | 112 | — | 0.97 |  |  |  | 152 |
| 19 | Zr20Ti20Hf20Be20Cu10Ni10 |  | 115 | — | 0.99 |  |  |  | 152 |

The ratios of the MGs to the base components (the subscript “bas”) and the component dominate electronic density of states at Fermi surfaces of MGs (the subscript “DOS”) in terms of elastic modulus, respectively, are given.

References

1.	Wang, W. H., Prog. Mater. Sci. (2012) 57, 487

2.	Wang, Z. X., et al., J. Alloys Compd. (2005) 388, 262

3.	Yu, P., et al., J. Mater. Res. (2006) 21, 1674

4.	Tarumi, R., et al., Phys. Rev. B (2007) 76, 104206

5.	Plummer, J. D., et al., J. Non-Cryst. Solids (2009) 355, 335

6.	Davis, L. A., et al., J. Appl.Phys. (1982) 53, 4834

7.	Pang, J. J., et al., J. Alloys Compd. (2013) 577, S56

8.	Chen, M. W., Annual Review of Materials Research, (2008) 38, 445

9.	Wang, W. H., J. Appl. Phys. (2012) 111, 123519

10.	Wang, W. H., J. Appl. Phys. (2006) 99, 093506

11.	Torrens-Serra, J., et al., Appl. Phys. Lett. (2013) 102, 041904

12.	Liu, Y., et al., Phys. Rev. Lett. (2009) 103, 065504

13.	Sheng, H. W., Acta Mater. (2008) 56, 6264

14.	Li, G. Q., Acta Mater. (2009) 57, 804

15.	Guo, M. L., Mater. Trans. JIM (2007) 48, 1717

16.	Wang, W. H., Prog. Mater. Sci. (2012) 57, 487

17.	Wang, X. D., Scripta Mater. (2011) 64, 81

18.	Wang, L., et al., Scripta Mater. (2011) 65, 759

19.	Senkov, O. N., and Scott, J. M., J. Non-cryst. Solids (2005) 351, 3087

20.	Wang, G. Y., et al., Metal. Mater. Trans. A (2011) 42, 1499

21.	Barney, E. R., Intermetallics (2011) 19, 860

22.	Senkov, O. N., et al., J. Alloys Compnds. (2006) 424, 394

23.	Calvayrac, Y., Phi. Mag. B (1983) 48, 323

24.	Liu, X. J., Phys. Rev. Lett. (2010) 105, 155501

25.	Mattern, N., et al., Intermetallics (2013) 32, 51

26.	Kwon, O. J., Mater. Sci. Eng. A (2007) 449, 169

27.	Mattern, N., J. Alloys Compnds. (2009) 485, 163

28.	Ott, R. T., Phys. Rev. B (2009) 80, 064101

29.	Park, K. W., Scripta Mater. (2007) 57, 805

30.	Eckert, J., Intermetallics (2006) 14, 876

31.	Baser, T. A., et al., J. Alloys and Compnds. (2009) 483, 146

32.	Mattern, N., Acta Mater. (2009) 57, 4133

33.	Xu, D. H., et al., Phys. Rev. Lett. (2004) 92, 245504

34.	Ma, D., et al., Nat. Mater. (2009) 8, 30

35.	Lu, B. F., et al., Intermetallics (2011) 19, 1032

36.	Wu, Y., et al., Sci Rep. (2015) 5, 10

37.	Das, J., Phys. Rev. Lett. (2005) 94, 205501

38.	Yu, P., et al., J. Non-Cryst. Solids (2005) 351, 1328

39.	Wang, X. D., J. Appl. Phys. (2008) 104, 093519

40.	Bednarcik, J., Mater. Sci. Eng. A (2008) 498, 335

41.	Calin, M., Mater. Sci. Eng. A (2005) 392, 169

42.	Calin, M., et al., Scripta Mater. (2003) 48, 653

43.	Kaban, I., Phys. Rev. B (2009) 79, 212201

44.	Inoue, A., et al., Nature Mater. (2003) 2, 661

45.	Hostert, C., J. Phys.: Condens. Matter (2011) 23, 475401

46.	Wang, W. H., J. Appl. Phys. (2006) 99, 093506

47.	Li, H. X., Scientific Report (2013) 3, 1983

48.	Stoica, M., J. alloys Compnds. (2010) 504, S123

49.	Shen, B. L., et al., Appl. Phys. Lett. (2004) 85, 4911

50.	Petkov, V., J. Non-Crystalline Solids (1995) 192, 65

51.	Yao, K. F., and Zhang, C. Q., Appl. Phys. Lett. (2007) 90, 061901

52.	Stoica, M., J. Alloys Compnds. (2009) 483, 632

53.	Stoica, M., et al., Phil. Mag. Lett. (2006) 86, 267

54.	Park, E. S., J. Appl. Phys. (2008) 104, 023520

55.	Zhang, Q. R., The Chinese Journal of Nonferrous Metals (2007) 17, 303

56.	Xi, X. K., et al., J. Non-Cryst. Solids (2004) 344, 189

57.	Wang, X. D., Appl. Phys. Lett. (2011) 98, 031901

58.	Zheng, Q., Scripta Mater. (2007) 56, 161

59.	Yim, H. C., Scripta Mater. (2006) 54, 187

60.	Schuh, C. A., and Nieh, T. G., J. Mater. Res. (2004) 19, 4

61.	Yim, H. C., et al., J. Non-cryst. Solids (2006) 352, 747

62.	Zeng, Y. Q., et al., Intermetallics (2010) 18, 1790

63.	Kawashima, A., Mater. Sci. Eng. A (2008) 498, 475

64.	Matsuura, M., J. Alloys Compnds. (2010) 496, 135

65.	Yao, K. F., et al., Appl. Phys. Lett. (2006) 88, 122106

66.	Chen, N., Acta Mater. (2009) 57, 2775

67.	Mattern, N., J. Non-Cryst. Solids (2004) 345, 758

68.	Hirata, A., et al., J. Alloys Comp. (2009) 483, 64

69.	Haruyama, O., et al., J. Non-Cryst. Solids (2007) 353, 3053

70.	Hufnagel, T. C., et al., Scripta Mater. (2000) 43, 1071

71.	Fan, C., Appl. Phys. Lett. (2006) 89, 231920

72.	Hui, X., Acta Mater. (2009) 57, 376

73.	Liu, Y. H., et al., Science (2007) 315, 1385

74.	Wang, X. D., Appl. Phys. Lett. (2007) 91, 081913

75.	Wang, X., Acta Mater. (2011) 59, 1037

76.	Zhang, Q. S., et al., Scripta Mater. (2006) 55, 711

77.	Bednarcik, J., J. Alloys Compnds. (2010) 504, S155

78.	Jiang, Q. K., Acta Mater. (2007) 55, 4409

79.	Li, S., et al., J. Non-Cryst. Solids (2008) 354, 1080

80.	Chou, C. P., et al., J. Appl. Phys. (1979) 50, 3334

81.	Chen, Y.-T., et al., Appl. Phys. Lett. (2013) 102, 051905

82.	Yao, J. H., et al., Appl. Phys. Lett. (2008) 92, 255506

83.	Park, J. M., et al., Appl. Phys. Lett. (2010) 96, 031905

84.	Chang, Z. Y., et al., Mater. Sci. Eng. A (2009) 517, 246

85.	Makino, A., et al., Scr. Mater. (2009) 60, 277

86.	Inoue, A., et al., Acta Mater. (2004) 52, 4093

87.	Petkov, V., J. Non-Cryst. Solids (1994) S192–193, 65

88.	Yao, K. F., and Zhang, C. Q., Appl. Phys. Lett. (2007) 90, 061901

89.	Stoica, M., et al., J. Alloys Comp. (2009) 483, 632

90.	Stoica, M., et al., Phil. Mag. Lett. (2006) 86, 267

91.	Liu, Y., et al., Appl. Phys. Lett. (2008) 93, 823

92.	Qiang, J. B., et al., Mater. Sci. Eng. B (2008) 148, 114

93.	Qiang, J. B., et al., J. Mater. Res. (2008) 23, 1940

94.	Shen, H. F., et al., Mod. Agric. Sci. Technol (2006) 2, 18

95.	Zeng, Y. Q., et al., Intermetallics (2010) 18, 1790

96.	Kawashima, A., et al., Mater. Sci. Eng. A (2008) 498, 475

97.	Matsuura, M., et al., J. Alloys Comp. (2010) 496, 135

98.	Xu, D., et al., Acta Mater. (2004) 52 (12), 3493

99.	Wang, J. Q., et al., J. Non-Cryst. Solids (2008) 354, 5440

100. Li, Z. G., et al., J. Alloys Comp. (2008) 454, 168

101. Duan, G., et al., Scr. Mater. (2008) 58, 465

102. Wu, X. F., et al., J. Alloys Comp. (2008) 452, 268

103. Qin, F. X., et al., Intermetallics (2008) 16, 1026

104. Wei, H. W., Prog. Mater. Sci. (2012) 57, 487

105. Peng, Y., et al., Hangkong Xuebao/Acta Aeronautica et Astronautica Sinica (2008) 29, 1

106. Das, J., et al., Phys. Rev. Lett. (2005) 94, 205501

107. Zhang, L., et al., Acta Mater. (2009) 57, 1154

108. Liu, Y. H., et al., Science (2007) 315, 1385

109. Zhang, Y., et al., Acta Mater. (2003) 51, 1971

110.	Xing, L. Q., et al., Phys. Rev. B (2001) 64, 607

111.	Zhang, Z. F., et al., Acta Mater. (2003) 51, 1167

112.	Lewandowski, J. J., et al., Phil. Mag. Lett. (2005) 85, 77

113.	Fan, C., et al., Appl. Phys. Lett. (2006) 89, 231920

114.	Hui, X., et al., Acta Mater. (2009) 57, 376

115.	Wu, Y., et al., Sci. Rep. (2015) 5, 12137

116.	Shen, B., et al., Appl. Phys. Lett. (2006) 88, 131907

117.	Wang, X. D., et al., Appl. Phys. Lett. (2007) 91, 081913

118.	Wang, W. H., et al., Mater.Sci. Eng. R (2004) 44, 45

119.	Johnson, W. L., JOM (2002) 54, 40

120. Duan, G., et al., Scr. Mater. (2008) 58, 159

121. Cheng, Y. Q., et al., Acta Mater. (2009) 57, 3253

122. Tarumi, R., et al., Phys. Rev. B (2007) 76, 104206

123. Li, P., et al., Mater. Sci. Eng. A (2009) 518, 16

124. Calvayrac, Y., et al., Phil. Mag. (1983) 48, 323

125. Liu, X. J., et al., Phys. Rev. Lett. (2010) 105, 155501

126. Park, K.-W., et al., Scr. Mater. (2007) 57, 805

127. Ma, D., et al., Nature Mater. (2009) 8, 30

128. Lu, B. F., et al., Intermetallics (2011) 19, 1032

129. Eckert, J., et al., Intermetallics (2006) 14 (8-9), 876

130. Baser, T. A., et al., J. Alloys Comp. (2009) 483, 146

131. Yu, P., et al., J. Non-Cryst. Solids (2005) 351, 1328

132. Wang, X. D., et al., J. Appl. Phys. (2008) 104, 093519

133. Bednarcik, J., et al., Mater. Sci. Eng. A (2008) 498, 335

134. Calin, M., et al., Mater. Sci. Eng. A (2005) 392, 169

135. Calin, M., et al., Scr. Mater. (2003) 48, 653

136. Inoue, A., and Zhang, W., Mater. Trans. (2004) 45, 584

137. Schroers, J., and Johnson, W. L., Phys. Rev. Lett. (2004) 93, 255506

138. Mukai, T., et al., Intermetallics (2002) 10, 1071

139. Liu, L., et al., Mater. Trans. (2005) 46, 376

140. Tarumi, R., et al., Jap. J. Appl. Phys. (2008) 47, 3807

141. Wada, T., et al., Mater. Sci. Eng. A (2007) 449, 958

142. Chen, H. S., J. Non-Cryst. Solids (1978) 29, 223

143. Johnson, W. L., and Samwer, K., Phys. Rev. Lett. (2005) 95, 195501

144. Li, S., et al., J.  Non-Cryst. Solids (2008) 354, 1080

145. Sheng, H. W., et al., Acta Mater. (2008) 56, 6264

146. Li, G., et al., Acta Mater. (2009) 57 (3), 804

147. Pang, J., et al., J. Alloys Compd. (2013) 577, S56

148. Liu, X. F., et al., Appl. Phys. Lett. (2007) 91, 041901

149. Li, Z., et al., J. Alloys Compd. (2008) 454, 168

150. Yu, H. B., et al., Appl. Phys. Lett. (2008) 92, 141906

151. Xi, X. K., et al., J. Mater. Res. (2005) 20, 2243

152. Gong, P., et al., J. Alloys Compd. (2020) 817, 153240